MEASUREMENT OF TRANSFORMATION TEMPERATURES OF Ni-Ti SHAPE MEMORY ALLOYS WITH USING METHODS CONTINUOUS CHANGE OF RESISTIVITY AS FUNCTION OF TEMPERATURE AND DTA

I. Szurman (a), M. Kursa (a)

(a) 	Faculty of Metallurgy and Materials Engineering, Technical University of Ostrava, 708 33 Ostrava, Czech Republic

# Abstract

System Ni-Ti is based on equiatomic compound of nickel and titanium. Ni-Ti based alloys are highly stable and resistant to corrosion. Production of these alloys is very difficult due to high reactivity of titanium. For successful use in practice it is very important to know transformation characteristics of these alloys. It is possible to measure transformation temperatures by deformation methods, by DSC, DTA or by resistometric methods. This article deals with method of continuous change of resistivity as function of temperature and DTA of Ni-Ti alloys, and with influence of deformation and subsequent heat treatment on these temperatures.

1. Introduction

Shape memory phenomena were observed for the first time at the beginning of the sixties in Ni-Ti based alloys. These alloys are characteristic by their structural arrangement at long distance, by thermoelastic martensite and crystallographically reversible phase transformation. In the system Ni-Ti special attention is paid particularly to intermetallic compound NiTi, which shows shape memory phenomenon. This phenomenon is, however, highly sensitive to stoichiometry of intermetallic phase TiNi, which is connected with specific requirements to metallurgy of these inter-metallic compounds [1]. Fabrication of alloys on the base of Ni-Ti is realized mostly by vacuum melting processes and plasma melting. Two the most commonly used techniques are vacuum arc melting and vacuum induction melting. Plasma melting can be used too [2].

2. Transformation in alloys Ni-Ti and measurement of transformation temperatures

Very string dependence of transformation temperatures on nickel contents in matrix has been proved. Chemical composition of materials and also heat and mechanical treatment is another initiator of modification of temperatures of phase transformation. Manner of treatment very significantly influences also scope of shape memory phenomena and magnitude of force, generated in the course of shape recovery. In Ni-Ti and Ni-Ti-Me(Cu) based alloys the following transformations take place:

- B2 ( B2 + B 19‘ (( B19‘‘), for TR( Mf

- B2( B2 + B19‘ ( R + B19‘( B19‘, for Mf < TR < Ms

- B2 ( R ( R + B19’,  for Ms < TR

- B2 ( B19 (  B19’ or B2 (  B19, for alloys Ni-Ti-Me(Cu).

Resistometric method enables simple, precise and rapid evaluation of transformation temperatures, and at the same time high quality reproducible results [3].

3. Experimental results

Samples in the form of drawn wire with diameter of 2.3 and length 60 mm have been used for measurement of transformation characteristics of the alloy Ni48.4- Ti51.6. Measurement was carried out on the original wire and afterwards on wires after various amounts of deformation, namely 9, 17 and 30%. We have subsequently investigated influence of heat treatment after deformation on transformation temperatures. Annealing was made at temperatures of 400 and 850°C with dwell of 1h. Cooling was performed freely in furnace atmosphere. D1 is designation of the sample, number in brackets gives amount of deformation and the next number gives possible heat treatment. Example of measured transformation temperatures is given in the Fig. 1. After that were carried out measurement of transformation temperatures with the use of DTA method. Specimens were cut from the wire and their length were 3 mm. We used dynamic atmosphere of He, purity 6N. Heating and cooling rate were 6 °C / min. Measured transformation temperatures are shown in table 1.

4. Conclusion

Resistometric method of measurement of transformation temperatures of Ni-Ti based alloys, as it is described above, was found to be a suitable method, namely thanks to its good reproducibility. DTA method confirms measured temperatures. Our working site at present concentrates on preparation of new types of alloys, their fabrication a monitoring their transformation characteristics.

5. Acknowledgement

The work presented in this paper was supported by the State Committee for Scientific Research (GAČR Grant No. 106/03/0231 „Vliv procesu přípravy paměťových materiálů Ni-Ti-Me na jejich strukturu a možnosti řízení jejich transformačních charakteristik“, which is gratefully acknowledged.

6. References

- Filip, P.: Fyzikálně metalurgické parametry tvarově paměťových jevů ve slitinách typu Ti-Ni a možnosti jejich využití, Kand. dis. práce, VŠB Ostrava, 1989, 163 s.

- WANG, LM., et al., Melting and Fabrication of NiTi Shape-Memory Alloy Wires,  Materials Science Forum, vol. 394-395, p. 297-300, 2002

- LORETHOVA, H. Strukturně fázová analýza slitin TiNi s tvarově paměťovými vlastnostmi pro lékařské aplikace. Dis. práce, VŠB Ostrava, 1997.

# Text boxes

Fig. 1 Measured transformation temperatures of alloy D1

| D1 | T [°C]R | T [°C]DTA |
| --- | --- | --- |
| TR [°C] | 78 |  |
| Ms [°C] | 61 | 65,9 |
| Mf [°C] | 30 | - |
| As [°C] | 82 | 79,87 |
| Af [°C] | 95 | 95 |
| H [°C] | 21 |  |

Tab. 1 Transformation temperatures of alloy D1